Methylene number of active carbon

The aim of the laboratory practice is evaluation of coloring agents removal from waste water efficiency.

INTRODUCTION

Methylene number is a parameter of active carbon (AC) which gives opportunity to indicate de-coloring properties of AC (sorption properties in solutions). Other analytical methods of sorption properties indication are exemplary:

Iodine number;

Phenol number;

Molasses number;

Detergent number;

pH number;

and it use depends on range of AC application.

“Methylene blue (CI 52015) is a heterocyclic aromatic chemical compound with the molecular formula C16H18N3SCl. It has many uses in a range of different fields, such as biology and chemistry. At room temperature it appears as a solid, odorless, dark green powder, that yields a blue solution when dissolved in water. The hydrated form has 3 molecules of water per molecule of methylene blue.” [1]

Caution:

“Methylene blue should not be confused with methyl blue, another histology stain, new methylene blue, nor with the methyl violets often used as pH indicators.” [1]

Fig. 1 Structural chemical formula of methylene blue [1]

Molar mass	319.85 g/mol (pure substance)

Molar mass	373,9 g/mol (hydrated by 3 molecules of water – typical commercial form)

APPARATUSES AND APPLIANCES

Spectrophotometer, cuvettes (absorption cells), laboratory shaker

GLASS AND CHEMICALS

Methylene Blue, active carbon, laboratory bulbs, laboratory flasks with stoppers, measuring pipettes

Measuring schedule

- Prepare base solution of the methylene dye by dissolving of 25 mg of the Methylene Blue in 500 cm3 of distilled water.

- Prepare the set of standard dye solutions:

  - to 7 measuring flask of 10 cm3 volume batch 0.05; 0.1; 0.2; 0.4; 0.5; 0.8; 1.0 cm3 of base solution and fill the flask to the mark using distilled water

  - calculate concetration of obtained solutions in mg/dm3

  - measure the absorbance A of standard solutions using wavelength =660 nm in the cuvette  of thickness of absorbing layer 1 cm

- Measure of cleaning effectiveness of dye solution by the active carbon

  - to the flask with with stopper of 100 ml volume sample 0.1 g of active carbon with accuracy of 4 fractional numbers (after the dot). Do two repeats (together 3 samples)  for the same carbon

  - Add the 50 cm3 of base dye solution. Shake the vessel on the laboratory shaker by the 60 minutes.

  - After shaking separate the solution using paper filter

  - Measure the absorbance A of the solution using wavelength =660 nm in the cuvette  of thickness of absorbing layer 1 cm

Data procesing

- Data on the absorbance of the standard dye solutions express on the chart absorbance versus concentration of the dye. Draw the line of tendency. In such a way the calibration curve appears.

- Using the calibration curve find the concentration of the solution obtained after adsorption on active carbon.

- Calculate the adsorption in g of dye per g of AC [g/g], this value is called methylene number.

Questions (short, several statement answer):

- Which property (or properties) plays role in sorption properties (especially adsorption)?

- Why silver coating is used for purification of drinking water?

Reference

[1] http://en.wikipedia.org/wiki/Methylene_blue (2012-11-03)