## Slide 1
NMR of manganites
Czesław Kapusta
AGH University of Science & Technology
Cracow, Poland

## Slide 2
Basic principles of NMR
  application to magnetically ordered state
Hyperfine field and its components
  information on the:
- valences, magnetic moments & T dependence
- magnetic coupling, phase segregation
- correlations, transitions (vs.T,B)
Nuclear relaxation
  information on magnetic (electronic) fluctuations

## Slide 3
Nuclear magnetic resonance (NMR):
nuclear magnetic moments n (I0) are probes for magnetic hyperfine fields (HFF) and nuclear quadrupole moments Qn (I>1/2) are probes for electric field gradients (EFG) at the nucleus
most of the elements have a useful (abundance) NMR isotope:
55Mn, 139La, 59Co, 17O ...........
- element (isotope) selective
- crystallographic (magnetic) site selective

## Slide 4
HFF, EFG  individual site properties
Fluctuations of HFF, EFG contribute to nuclear relaxation, T1, T2  dynamics
Nuclear magnetic resonance (NMR):
magnetic moment of open electronic shells  HFF
asphericity of open shells  EFG

## Slide 5
  Nuclear magnetic moment n is related to the nuclear spin I:
    where n is the nuclear gyromagnetic ratio.
    For 55Mn n corresponds to 10.55 MHz/Tesla
    where mp - proton mass, e – elementary charge
    Energy levels of nuclear spin in a magnetic field B0 are:
    m = -n  B0 m (3)
    where m runs from –I to I
    Nuclear moments are of the order of nuclear magneton:

## Slide 6
    E.g. for I= ½ - two levels, nuclear magnetisation proportional to the difference of their population.
    Occupation probability: Boltzmann distribution - nuclear magnetisation equals:
    where  = 1/kBT ,  = nB0 , n - number of nuclei/m3.
    High temperature condition, 1, usually fulfilled, so that:
     nuclear paramagnetism

## Slide 7
    Generally for a nuclear spin I we have:
    NMR signal induced in a probe coil is proportional to the nuclear magnetisation and thus depends on:
    - concentration (amount of the element in the coil),
    - abundance of the NMR isotope,
    - gyromagnetic ratio,
    - spin
    and the frequency of the resonance (signal induced in the coil)

## Slide 8
Relative intensities of NMR signals of different isotopes roughly compare with their „NMR sensitivity”
- at constant field:
- and at constant frequency:

## Slide 9
    Nuclear relaxation
    spin - lattice
    In an NMR experiment T1 can be determined e.g. from saturation recovery
    If initially M=0 and the field B0 is applied at t=0, nuclear magnetisation increases according to the equation:
    T1 is the spin-lattice relaxation time
    it usually varies between microseconds and seconds, depending on the material and temperature

## Slide 10
  Semi-classical description of NMR
  - nuclear magnetisation precessing around the magnetic field B0||z
    In an isotropic magnetic field nuclear moments precess according to the equation:
    Equation (8) can be transformed from the laboratory frame to the frame rotating around z-axis with angular frequency ’. In this frame magnetic field equals:

## Slide 11
    So that for:
      ’ = 0 = n B0 (12)
      nuclear moments „do not see” the external field B0 – they „rest” in the rotating frame.
Angular frequency transformed to the laboratory frame equals:

## Slide 12
    and the resonant frequency:
    - basic equation of NMR - resonant frequency is proportional to the field at nucleus

## Slide 13
  Spin echo method
    Linearly polarised (radiofrequency - r.f.) field due to alternating current in the probe coil corresponds to two circularly polarised fields of opposite helicities:
    One of the fields rests in the rotating frame x’y’z’, the other rotates with angular frequency 20 and does not contribute to the resonance. The field in the rotating frame is:

## Slide 14
    At the resonance it simplifies to:
    Let’s start from the situation with M=M, M||z and consider evolution of nuclear magnetisation in the rotating frame (x’y’z’|0) during a pulse i :
    - spins „see” only the field B1 parallel to the pulse axis (here x’)
- M is precessing about B1 with angular frequency nB1 in the plane zy’ and the turning angle amounts to:
    B1 and i are adjusted to get a desired rotation angle, most often /2 and  (/2 and  pulses).
(18).

## Slide 15
A scheme of free induction decay and spin echo formation
(a). /2 pulse - nuclear magnetisation rotates to the x’y’ (xy) plane and produces FID signal
(b). Nuclear magnetisation forms a „fan” due to a distribution of B0 in the sample
(c). Inverting  pulse swaps slower spins with „faster” spins
(d). First echo
(e). A subsequent inverting  pulse swaps slower spins with „faster” spins
(f). Subsequent echo

## Slide 17
    Pulse  compensates the influence of local inhomogeneities, provided they are not time dependent. Time dependence of echo amplitude is influenced by relaxation processes (in liquids also by difussion) which cause random changes of phases of individual nuclear spins.
    The spin echo decays with time in te same way as the in-plane component of nuclear magnetisation in an ideally homogeneous field:
    where T2 is the „transverse” relaxation time.
    As this relaxation originates mostly from (indirect) interactions between nuclear spins, T2 is usually called spin-spin relaxation time.
(20)
Bloch equations - motion of nuclear magnetisation:

## Slide 18
    Integration of the Eq. (18) gives the time dependence of the transverse magnetisation and the spin echo:
    where t starts at the /2 pulse.

## Slide 19
    For the /2 -  pulse sequence t approximately equals 2  pulse separation.
    T2 can be determined from a measurement of echo intensity vs pulse separation.
NMR time window: 1) Larmor ~ 10-6 - 10-9 s
in spin-echo also: 2) > 2 (T2) ~ 10-5 s

## Slide 20
NMR in magnetically ordered materials
  Hyperfine interactions

## Slide 21
  Effective field at nucleus
    In a magnetically ordered material the effective magnetic field at nucleus can be conveniently expressed as a sum:
    Be = BF + Borb + Bdip + B0 (24)
    where: BF – Fermi contact term
    Borb – orbital term
    Bdip – dipolar term
    B0 – external field
    The sum of BF and Borb is usually called hyperfine field, Bhf
    where: (0) , (0) – spin up and spin down s-electron density at nucleus
    ((0) – (0)) – spin polarisation at nucleus

## Slide 22
  In the magnetic S-state ions or with orbital moment quenched Fermi contact term due to the own spin moment is dominant and antiparallel to the magnetic moment.
  A field at nuclei of „nonmagnetic” ions can originate from polarisation of their electrons by magnetic neighbours and/or from dipolar fields.
  Fermi contact field from core s-electrons is related to the spin moment of the ion:
  where β is the hyperfine coupling for the orbital moment of the element.
  where α is the hyperfine coupling for the spin moment and is of order of 10 T/B for 3d (e.g. Mn), 40 T/B for 4d and 100 T/B for 5d elements (I.A.Campbell).
  Also the orbital field can be expressed as:

## Slide 23
    In a ferro or ferrimagnetic material an r.f. field of amplitude B1 tilts electronic magnetisation at an angle  (proportional to r.f. susceptibility) from the direction determined by a sum of anisotropy field and external field Bc. This causes a corresponding tilting of Be and the appearance the in-plane r.f. field Be >> B1 of the amplitude:
  Enhancement of the r.f. field
Illustration of the enhancement in a magnetic domain

## Slide 24
     is termed the NMR enhancement factor, for domain interiors (DI) it amounts 10 – 103. In the domain walls (DW)  can be 10 – 100 times larger. Both signals can be observed and the resonant frequencies (Be) can differ. DW signals have usually shorter T2 than DI signals. DW and DI signals can also be distinguished by application of magnetic field.
     in antiferromagnets is much smaller than in ferro- and ferrimagnets and field independent. In ferro- and ferrimagnets it decreases with increasing field.
    Owing to the enhancement effect the pulse power required in NMR of magnetically ordered materials is 2 times smaller than in dia- or paramagnetics and the echo amplitude is  times larger.

## Slide 25
Nuclear relaxation
Longitudinal and transverse relaxation rates can generally be expressed as:
where f1 and f0 are the correlation functions of transverse and longitudinal fluctuations of the field at nucleus, respectively.
1/T1 is determined by the Fourier component of transverse correlation function at  = n whereas 1/T2 includes also contribution from the whole spectrum of longitudinal fluctuations.
Fluctuations in the electronic and lattice subsystems produce fluctuating fields (and EFG) which cause relaxation of nuclear magnetisation
(31)
(32)

## Slide 26
Typical dependence of relaxation rates on the correlation time (an example for rotational fluctuations)
For short correlation times relaxation rates are similar

## Slide 27: NMR3 - Magn. ordered materials
For magnetic ions: Be~ <μz>
 ionic states with different moments can be distinguished
Be(T) ~ <μz(T)>
 temperature dependence of local magnetisation can be obtained
For the S-state or quenched orbital contribution:
Be ~ <Sz>
 value of the spin moment can be determined
Magnetically ordered materials:
- broad lines due distribution of hyperfine fields (domain walls, defects), linewidth  1/T2
 frequency swept spin echo most useful

## Slide 28
Phase diagram of La1-xCaxMnO3
J.L. Martinez, J. Magn. Magn. Mater. 196-197 (1999) 520.

## Slide 29
Valences & magnetic moments 55Mn spectra at 4.2K
single line x=0.33, 0.45 - fast electron hopping (DE) (h<<L)
the DE line at 380 MHz (37T) appears also in x=0.1 in addition to the 4+ line at 318 MHz (31 T) and 3+ resonance at 400 - 550 MHs (39-54 T)
 FM metallic DE clusters
the DE clusters’ line appears also for x=0.65 and 0.75 at 375 MHz, in addition to the Mn4+ (AF) line at 290 MHz
Difference of Be in FM and AF: dipolar and transferred HFF (Ga NMR, C.Oates)
Cz. Kapusta, P.C. Riedi, W. Kocemba, M. R. Ibarra, J.M.D. Coey, J. Appl. Phys. 87 (2000) 7121.
distinct 4+, DE and 3+ states (Be ~ Mn)

## Slide 30: Valences & magnetic moments
Mn4+: 290-330 MHz  29 - 32 T (Fermi contact + transferred),  = 10 T/B  spin moment 3 B
DE: 370-390 MHz  36 - 38 T (Fermi contact + transferred)  spin moment 3.6-3.8 B
Mn3+: 400-520 MHz  39 - 51 T (Fermi contact + orbital + transferred)  spin moment of 4 B, orbital moment of 0.2 B

## Slide 31
Valences & magnetic moments
La0.9Ca0.1MnO3 NMR spectra, FMI
P.A. Algarabel et al. PRB (2003)
The DE line at 380 MHz appears also in x=0.1 in addition to the lines at 318 MHz (Mn4+) and 435 MHz (Mn3+)
 FM DE clusters in the FMI matrix  phase segregation
The DE line and the FMI lines exhibit different temperature evolution of their intensities, hyperfine fields and nuclear relaxation times

## Slide 32
Temperature dependence of Be
Be (<Sz>) within the DE clusters exhibit a weaker temperature dependence and does not vanish at TC (TN) in contrast to Be (<Sz>) in the host (AF) matrix
The Be (<Sz>) in the DE clusters is less temperature dependent for the hole doped than for the electron doped compounds
Different strength of the magnetic coupling in the FM and FI (AFI) regions
Different strength of coupling between FI and FM (AF) regions
Cz. Kapusta, P.C. Riedi, W. Kocemba, M. R. Ibarra, J.M.D. Coey, J. Appl. Phys. 87 (2000) 7121.

## Slide 33
Phase segregation FMI/FMM
La0.9Ca0.1MnO3
RESULTS
P.A. Algarabel et al. PRB (2003)
Be La is of 3 - 5 Tesla
Phase segregation is also seen in the La NMR spectra (4.2 K) where two lines corresponding into FM metallic (lower peak) and FM insulating (upper peak) phases are observed
A stronger Mn 3d - La sp overlap in the FMI phase can be deduced

## Slide 34
Phase segregation AFI/FMM La0.35Ca0.65MnO3 55Mn spectra optimum pulse power set at the upper line
290 MHz line -small enhancement, broadens, not shifts in the applied field  AF regions (4+)
Cz. Kapusta, P.C. Riedi, M. Sikora, M. R. Ibarra, Phys.Rev. Lett. 84 (2000) 4216.
375 MHz -large, field dependent enhancement, shift in the applied field  FM regions ~83% in the AF CO matrix
RESULTS

## Slide 35
FM metal & DE cluster glass 55Mn spectra
La0.67Ca0.33MnO3, La0.7Sr0.3MnO3
- metallic FM
RESULTS
single line
- fast hole hopping
(DE) (h << Larmor = 10-9 s)
La0.6Y0.07Ca0.33MnO3
- max. CMR effect
La0.67-yTbyCa0.33MnO3 y>0.2
- cluster glass insulator
Cz. Kapusta et al., J. Phys.: Condens. Matter 11 (1999) 4079.

## Slide 36
Magnetic (DE) polarons
in the compounds with low TC (Tg) the zero field NMR signal observed at
T > TC or Tg corresponds to clusters of DE coupled Mn spins
long lived magnetic (DE) polarons (c>10-4 s)
Cz. Kapusta et al., J. Phys.: Condens. Matter 11 (1999) 4079.

## Slide 37
Character of magnetic transition La0.57Tb0.1Ca0.33MnO3 FM (TC = 160 K) Temperature dependence of M, I and Be
Be (<Sz>) has 90% of its low temp. value at TC (in "normal" ferromagnets it tends to zero)
T1 and T2 do not change on crossing TC
(a lack of any critical behaviour)
Signal intensity I follows the magnetisation
 amount of DE regions tends to zero at TC (1st order like)
Cz. Kapusta et al., J. Phys.: Condens. Matter 11 (1999) 4079.

## Slide 38
DE strength
lower Tc corresponds to a stronger temperature dependence of Be (<Sz>) and, thus, to
a weaker DE interaction
the compounds with lower TC exhibit a 1st order magnetic transition at TC
For the compounds with high Tc
the transition is of the 2nd order

## Slide 39
Field induced I-M transition Pr0.7Ca0.3MnO3 55Mn spectra at 3K
AF, CO, 1st order I-M transition in the applied field Y. Tomioka et al., J. Phys. Soc. Jpn., 64 (1995) 3626.
distinct 4+, DE and 3+ states
up to 5T, slight increase of the population of DE regions at the cost of the 4+ and 3+ states
a collapse to a single line at
Bext>5T - transition to a metallic ferromagnet (a full  shift)
C. Kapusta, P.C. Riedi, J. Magn. Magn. Mater. 196-197 (1999) 446.
 1st order transition (hysteresis)

## Slide 40
Microscopic nature of CMR effect (increase of the population of DE regions in the applied field)
55Mn NMR spectra of Sm0.55Sr0.45MnO3

## Slide 41
55Mn NMR spin echo spectra of La1.4Sr1.6Mn2O7
Phase segregation
FMM La1.4Sr1.6Mn2O7
FMM and FMI regions at T< 110 K
DE clusters present up to at least 250 K

## Slide 42
Temperature dependences of T1 and T2 for the 4+ and DE lines
Nuclear relaxation
minimum of T1 at 90-120 K, where FMI phase disappears (turns paramagnetic)
 interplay of the fluctuations in the FMI phase with FMM phase
 nanoscopic phase segregation
FMM La1.4Sr1.6Mn2O7

## Slide 43
Conclusions
NMR in magnetically ordered state provides an information on:
valences, magnetic moments & T dependence
magnetic coupling, phase segregation
correlations, transitions (vs.T,B)
magnetic (electronic) fluctuations
In particular we could learn that in manganates:
FMM and FMI (AFI) “segregated” phases exhibit different strength of magnetic coupling,
CMR and magnetic field induced I-M transition correspond to the growth of population/size of FMM regions (DE clusters),
Bulk magnetic measurements provide ordering temperatures which are usually„blocking temperatures” of the superparamagnetic- like DE clusters, not the true Curie temperatures.
FINISH